## Slide 1: Yield Surface Fitting of Raw DP980 specimens
Thein Lin Aung, Kohki Enomoto, Ninshu Ma
JWRI, Osaka University
2023/02/24

## Slide 2
Hill48
M&A quadratic
Independent equivalent stress values
Independent equivalent stress values
Yield curve fitting of uniaxial and biaxial tensile tests
Rx = 1.0
Ry = 0.98
Rxy = 0.99
Rz = 1.0
Uniaxial tests from Honda (1.6 mm specimens)
Biaxial tests from TUAT (0.8mm specimens)

## Slide 3
Hill48
M&A quadratic
Equivalent stress for the yield curve was calculated from Swift equation of Raw L (Honda’s 1.6mm specimen)
Isotropic hardening is assumed, so YF parameters do not change.
Equivalent stress from Swift equation (Raw L)
Equivalent stress from Swift equation (Raw L)
Rx = 1.0
Ry = 0.98
Rxy = 0.99
Rz = 1.0
Yield curve fitting of uniaxial and biaxial tensile tests 2

## Slide 4
K | 1447
ep0 | 2.74E-05
n | 0.102
Bad Swift fitting accuracy at small strains
The Swift curve’s fitting accuracy is not good for small strains.
If fitting is optimized for small strains, large error occurs at large strains.

## Slide 5: Comparison of Raw L uniaxial SS-curves with 0.8mm large tensile specimen from JFE
K | 1447
ep0 | 2.74E-05
n | 0.102

## Slide 6: Modification of Swift parameters to fit JFE specimen’s SS-curve
K | 1668
ep0 | 1.374E-04
n | 0.1388
K | 1578
ep0 | 1.577E-04
n | 0.1343

## Slide 7
Rx = 1.0
Ry = 1.03
Rxy = 1.0
Rz = 1.0
Better fitting accuracy at small strains using optimized Swift parameters (JFE 2)
K | 1668
ep0 | 1.374E-04
n | 0.1388
Hill48
M&A quadratic

## Slide 8
equv. plastic strain
loading history variable
Uniaxial hardening curves
Yield function parameters
Return mapping
Equivalent stress and flow rule
Time step ++
State update
Pre-strain dependent anisotropic hardening (State variables update flow)

## Slide 9: Simulation: 3-point bending model using Isogeometric Analysis (IGA)
Experiment data (Stroke, displacement, strain) and material properties
CAD model => IGA model =>Elastoplastic bending simulation